MSc Project Abstracts 2008/9

1. On the Sensitisation of Austenitic Stainless Steels

Project Supervisor: Dr M Whiting

The so-called sensitisation of stainless steel has been known since the early days of their exploitation as engineering materials. The ‘textbook explanation’ of grain boundary depletion of chromium as the cause of sensitisation (i.e. a catastrophic reduction in corrosion properties) was proposed by Bain et al (1933). However, it was only in 1977 that Pande et al produced direct evidence of the depletion of Cr at the grain boundaries.

Contrary to many textbooks there is still significant uncertainty over the details of the mechanism of sensitisation. Even if chromium depletion explains all cases of sensitisation there is uncertainty as to the detail. For example, whether the magnitude of depletion or the width of the depleted zone is dominant is disputed.

This project will explore this basic phenomenon as applied to either (i) nitriding of stainless steel or (ii) in-service temperature excursions. The choice will be an informed one made by the student after about 1 month of background reading and discussion.

Whichever direction is chosen the work will necessitate the design of experiments and a programme of investigation which will include heat treatment, corrosion testing, optical metallography, scanning electron microscopy, transmission electron microscopy and possibly some tensile testing.

Bain, E. C., Aborn, R. H. and Rutherford, J. J. B., Trans. Am. Soc. Steel Treating 21, 481 (1933).

Pande, C. S., Sumagu, M., Vyas, B. and Isaacs, H. S., Scripta Met. 11, 681 (1977).

Recommended Modules: Physical Metallurgy, Materials Under Stress

2. The Interface Chemistry of Nanocomposite Materials

Project Supervisor: Prof. J F Watts

There is increasing interest in the performance of nanocomposite materials for structural applications, and many manufacturers are actively investigating modifying polymer resins in this manner to obtain improved performance for coatings, adhesives and fibre composite matrix applications.  Work has been carried out on these systems over the last decade in JFW’s Research Group.

The reinforcement phase in such materials is generally inorganic nanoparticulates in the size range 50-250 nm, and the performance of the composite material is critically dependent on the level of adhesion that is obtained between the reinforcement and the polymer resin matrix.  This work will explore the surface characteristics of nanoparticles for use in a polyurethane resin for commercial applications.  The work programme will be based around the characterisation of the surface thermodynamic properties of reinforcement and matrix by inverse gas chromatography(IGC) and the surface chemical properties by X-ray photoelectron spectroscopy (XPS) and time-of-flight secondary ion mass spectrometry (ToF-SIMS).  From a knowledge of these surface properties it will be possible to model the interface chemistry of these systems.  This will then be examined experimentally using a purpose built controlled strain rate fracture stage on our ToF-SIMS systems.  This stage allows miniature compact tension test pieces to be fractured in the ultra-high vacuum of the spectrometer and analysed without exposure to the ambient, thus preventing obliteration of the chemistry of failure by the deposition of adventitious material adsorbed from the atmosphere.

Recommended modules:  Surface Analysis, Science of Adhesion

3. The Effect of surface passivation on the performance of single crystals CdZnTe radiation detectors for medical and space applications.

Supervisor:  Dr Mark Baker, Dr Ersin Ozsan (Physics)

CdZnTe (CZT) single crystals are used for the fabrication of pixellated radiation detectors for X-ray medical imaging and gamma-ray spectroscopy in space.

The detector device characteristics are controlled by bulk and surface properties. At present Bromine Methanol (BM) etching is used to prepare surfaces which leaves behind a Te-rich surface. Pixellated devices are then prepared by evaporating Au or Pt as contacts. Part of the process then involves passivating this Te-rich surface with H2O2 dipping to form TeO2 (native oxide) insulating layer between the pixellated cells to minimize surface conduction. The aim here is to improve the detector performance by increased passivation with other chemical recipes e.g., NH4F, H2O2, KOH etc. In this project, effects of various surface treatments on detector performance will be investigated. (i) XPS analysis and depth profiling will be used to determine the chemistry and the thickness of oxide layers. (ii) Surface morphology will be determined by SEM and AFM, (iii) Metal / CZT interface will be investigated by SIMS and AUGER depth profiling. (iv) Detector devices will be fabricated using photolithography to measure current-voltage characteristics.

Recommended modules: Surface Analysis, Scanning Probe Microscopy, Introduction to Nanotechnology etc.

4. Initial measurements on the use of Auger electron spectroscopy to study non-conducting materials

Supervisors:  Prof John Watts, Dr Mark Baker

Auger electron spectroscopy is a surface analysis technique employing an electron source as an incident beam. On non-conducting samples, the technique suffers from surface charging and analysis of such materials is at best difficult and often not possible at all. Ion guns are fitted to Auger spectrometers to sputter the surface, enabling surface contamination to be removed or compositional depth profiling to be undertaken. The latest ion guns have a novel capability to bombard the surface with very low energy ions. This new functionality opens up the possibility of using low energy ions to neutralise the surface charging of non-conducting samples. In this project, materials with varying conductivities will be examined under different charge neutralising conditions. Using the new Microlab 310 instrument in the Surface Analysis Laboratory, the optimum experimental conditions (electron/ion beam energy, flux etc.) for each material will be established and the required conditions correlated with the material conductivity.

Recommended modules: Surface Analysis, Ceramic and Ceramic Matrix Composites

5. Characterisation of Advanced Ceramics

Supervisors: Dr Julie Yeomans, Dr Vlad Stolojan

The relationships between processing, microstructure and properties are central to the study of materials science and engineering.  In many ceramic materials, very small parts of the microstructure can control the macroscopic properties e.g. microscopic flaws control strength and grain boundary phases can dominate creep properties.  In this project, the aim is to explore the extent to which electron microscopy and spectroscopy can be used to characterise a number of different aspects of ceramic microstructures.  Initially, two case studies will be used: the first relates to defects (surface mottling) in commercially produced alumina components and the second to grain boundary chemistry and structure in a novel nanoceramic.

The student will be expected to become familiar with a range of scanning and transmission electron microscopy techniques although previous experience of these is not necessary.

Recommended modules: Characterisation of Advanced Materials (guided study), Ceramics and Ceramic Matrix Composites

6. Mechanical properties of hybrid carbon nanotube-fibre composites

Supervisor:  Dr Tina Lekakou

The presence of nanoparticles and carbon nanotubes in particular may improve the mechanical performance of a composite material, although not always to the expected level and sometimes mechanical properties actually get worse. This project includes manufacture of hybrid carbon nanotube-glass fibre composites, mechanical testing and microstructural investigations of the fractured surface or of the distribution of carbon nanotubes.

Recommended modules:

7. Composites derived from natural fibres and eco-resins

Project Supervisors: Prof Paul Smith, Dr David Jesson

(Dr. Gavin Creech and Ms Angie Ellis, Scott-Bader).

As concern for the environment increases there is some interest in using natural fibres, particularly those which form waste products from other industries, to produce composite materials that can be used in non-critical applications.  If these can be combined with so called eco-resins then it may be possible to produce an extremely ‘low carbon’ material.

The current project will compare natural materials from two different sources (fibrous waste products from the palm oil and seed oil industries) and establish (with reference to international standards) methodologies for determining the mechanical properties (e.g. Young’s Modulus, tensile strength and strain-to-failure) of these fibres (and their subsequent composites).  It is anticipated that the fibres will undergo some form of processing so that they can be incorporated into a resin system and this, together with some form of dispersion method will form the second strand of research.  Finally a range of surface analytical techniques will be applied to determine the chemical properties of the fibre and if possible the likely form of interaction between the fibre and the matrix.

In summary, a range of novel composites will be produced and tested using natural fibres as a dispersed phase and an eco-resin as the matrix.

Recommended modules: Introduction to Composite Materials, Materials Under Stress, Surface Analysis.  The Science of Adhesion, Polymers for Advanced Applications may also be of interest.

8. Rapid evaluation of glass/polyester composites for toughness and durability

Supervisors: Dr Steve Ogin, Prof Paul Smith

The successful use of composite materials in some industrial sectors, such as the large scale use of GFRP in pipe manufacture (the subject of this project) would benefit from rapid tests to assess the performance of different glass and resin combinations.

This project will build on the successful MSc project carried out last year which began to look at ways to distinguish rapidly between such materials, using fracture mechanics tests.  The project will again be carried out in close collaboration with Dr Jane-Thatcher Haaveldsen of the major international pipe manufacturer, Flowtite Technology AS, Norway.

In the current project, fracture toughness testing, such as double-cantilever beam experiments, will be carried out on two candidate material combinations of interest to Flowtite.  In addition, it is proposed to manufacture and test simple cross-ply laminates from the two materials in order to instigate the possibility of using the accumulation of matrix cracking damage in such laminates as one means of discriminating rapidly between the candidate materials. It is also possible that some surface science techniques will be used to understand the fracture behaviour.

Recommended modules: Introduction to Composite Materials, Materials Under Stress, Surface Analysis (possibly)